## Slide 1: CDW management outside EU: best practices in Taiwan
Mike Hwang / NTUST

## Slide 2
University of Illinois at Urbana-Champaign, USA Ms. & PhD.
Distinguished Professor in National Taiwan University of Science and Technology
Director of SUS-CON Research Center, Taiwan Building Technology Center.
Professor Chao-Lung Hwang
Phone: (02) 27376575
Mobile: 0986604755
Email: Mikehwang@mail.ntust.edu.tw

## Slide 3
NTUST
Outline of presentation
Overview of CDW
Some major activities in Taiwan
Research results
1.
2.
3.

## Slide 4
Overview of CDW
Construction demolished waste
CLSM
HPC
Using AI method to design
Crushed aggregate
Green concrete
Useless material
Recycling aggregate

## Slide 5
Overview of CDW
Manufacturing processes of CDW

## Slide 6
Major Activities in Taiwan
Modeling the concrete strength using big data cloud-based symbiotic organisms search-least squares support vector machine
Study of recycled concrete aggregate (RCA) to produce HPC for environmental sustainability
Performance of controlled low-strength material (CLSM) and its application to highway construction
1
2
3

## Slide 7: Part 1 (BIG DATA)
Prediction of fresh and hardened properties of concrete and optimizing concrete mixture by SOS-LSSVM

## Slide 8
Research Objectives
Developing the model for predicting properties of HPC in term of compressive strength, workability and durability
Identify the optimum HPC mixture, with lowest cost and satisfy the requirement of compressive strength, workability and durability

## Slide 9
MODEL ARCHITECTURE
Slump, compressive strength and electrical resistivity properties prediction model
Input data

## Slide 10
OPTIMIZATION MODEL ARCHITECTURE
Optimizing concrete mixture model

## Slide 11
System Interface for Optimum HPC mixture
1
2
3
4
5
8
7
9
6
11
12
10
The users can decide the value of desired compressive strength, slump and electrical resistivity, the tolerance and the unit price of each component. The boundary of each ingredients is obtained from dataset. The value of population size and number of iteration are recommended in the model in order to obtain the best result.

## Slide 12: Part 2: 1. Utilization of CDW as aggregate to produce HPC
High performance recycled aggregate concrete

## Slide 13
Overview of DMDA
DMDA method

## Slide 14
DMDA Mix Design
14
Vp= Vv+ S*t=n*Vv
Vp:Paste volume
S:Particle surface area
t: Thickness
Vv:Void volume
n: amplification factor(1.1~1.5)
Aggregate stage :
1. Fly ash fills sand → maximum accumulation point (α),
2. (Flying ash + sand) fill stone → maximum accumulation point (β) → maximum unit weight of aggregates
Paste stage:
1. The ratio of the coarse and fine aggregate is fixed and freely adjusted.
2. Cement paste value (W/B) or amount (Vp).
Fly Ash
Coarse aggregate
Fine aggregate

## Slide 15
Blend aggregate
15
NFA
RFA
Fly ash
NCA
RCA
α1- α1 α1+
Volume of coarse aggregate
β1- β 1 β 1+
α1- = 30% α1 = 40% α1+ = 50%
β1- = 30% β1 = 40% β1+ = 50%
+10%
-10%
+10%
-10%
Recycled coarse aggregate replacement
Recycled fine aggregate replacement
Volume of fine aggregate
Using RA to replace to NA from 30-80% by volume

## Slide 16
Compressive strength development Different proportion of CDW content as aggregates
16
DMDA
NFA
RFA
FA
RCA
NCA
Compressive strength ranged 25-50MPa at 28 days with different CDW content and w/b
Good durability with high UPV value (>3660m/s); ESR result (>20KΩ-cm) and RCPT analysis (Qs<2000 coulomb)
Low cement content (<300kg/m3)

## Slide 17
Significant effect of DMDA on properties of HPC
↑0.49%
↑4.81%
↑2.22%
↑13.18%
↑0.02%
↑2.13%
↑0.38%
↑1.41%
40% CDW  significant improvement on strength and UPV
Using RCA more significant than RFA
Compressive strength at 28-days
UPV at 28-days

## Slide 18: NTUST-2: 2. Utilization of red brick and ceramic waste to produce mortar specimens

## Slide 19
Production of waste brick and ceramic sand and powders
Brick/ceramic Powder passing through #200 sieve
Granular brick/ceramic waste after gridded by Rolls crasher
As received brick/ ceramic collected from C & D debris site

## Slide 20
Paste production from brick and ceramic powder
Brick (or ceramic) powder content: 60%
Total slag and fly ash content: 40% with changing of slag from 10%, 20% and 30%
Compressive strength of 50-70 MPa is measured for brick powder and 30-45 Mpa for ceramic powder

## Slide 21
Mortar production from brick powder and ceramic sand
The GGBFS was used from 10-50% by weight of brick powder
Ceramic sand was used as fine aggregate
Compressive strength ranges 24-93 Mpa with 90-50% brick powder content
Natural aggregate

## Slide 22: NTUST-3 (CLSM)
Performance Characteristic of Controlled Low Strength Material (CLSM) Incorporating Construction Waste Applied to Highway Engineering

## Slide 23
Overview of CLSM
Reuse the construction demolish waste as aggregate for CLSM
Require high flowability and low compressive strength
CLSM
No useless material

## Slide 24
Slump flow and tube flow of CLSM
Slump flow test
Tube flow test
CDW content (%) | Slump flow (mm) | Tube flow (mm)
0 | 600 | 240
33 | 550 | 200
66 | 455 | 190
100 | 385 | 130
Higher CDW content  reduce the slump flow and tube flow
Reduction

## Slide 25
Using the CDW to produce CLSM
CDW content
CDW content
Using 100% CDW show light reduction of compressive strength compare with Natural aggregate
Compressive strength almost reach 8MPa at 28 days
CDW content

## Slide 26: Demo-site (EGA House)
EGA House

## Slide 27
Panels positon
Demo-site installation at EGA House
Panel dimension: Height: 3.1 m; Width: 1.2 m; Thickness: 0.15 m

## Slide 28
Concrete design from Construction Demolish Waste
CONCRETE was designed with 40% recycled sand and recycled coarse aggregate from CDW to replace to natural aggregate
The CDW concrete mix-design for 30MPa at 28 days (kg/m3)
Steel mold before casting concrete
Concrete panel

## Slide 29
Observation for panel installation at EGA House

## Slide 30: NTUST- publications
Chao-Lung Hwang, Mitiku DamtieYehualaw, Duy-Hai Vo, Trong-Phuoc Huynh, Alessandro Largo (2019). Performance evaluation of alkali activated mortar containing high volume of waste brick powder blended with ground granulated blast furnace slag cured at ambient temperature. Construction and Building Materials 223: 657-667 (SCIE).
Chao-Lung Hwang, Mitiku DamtieYehualaw, Duy-Hai Vo, Trong-Phuoc Huynh (2019). Development of high-strength alkali-activated pastes containing high volumes of waste brick and ceramic powders. Construction and Building Materials 218: 519-529 (SCIE).
Duy-Hai Vo, Chao-Lung Hwang, Khanh-Dung Tran Thi, Mitiku DamtieYehualaw, Wei-Chih Chen. Effect of reactive MgO on the engineering properties and durability of high-performance recycled aggregate concrete-based alkali-activated slag and fly ash. (finished revise to submit).
Duy-Hai Vo, Chao-Lung Hwang, Khanh-Dung Tran Thi, Mitiku DamtieYehualaw. The significant effect of recycled fine aggregate and fly ash content on the alkali-activated slag-MgO mortar. (finished revise to submit).

## Slide 31: Thank you for your attention
Chao-Lung HWANG (Mike)
mikehwang@mail.ntust.edu.tw