## Slide 1: The recycling of buildings materials
Linus Brander, RISE

## Slide 2: Construction Demolition Waste - CDW
25% - 30% of all waste generated in EU
Mixture of concrete, bricks, gypsum, wood, glass, metals, plastic, solvents, asbestos, excavated soil, etc.
Source: construction of buildings and civil infrastructure, total or partial demolition of buildings and civil infrastructure, road planning and maintenance
Low recycling levels!
Prefabrication industry: up to 50% less waste than conventional construction practices

## Slide 3: Some of the objectives in RE4
Development of prefab. elements integrating a high level of CDW-derived materials
Development of innovative design concepts for pre-fabricated building components
RE4 demonstration in industrial environment, testing and evaluation, replication

## Slide 4: Achievement: Prefab elements constituting 30-95 % CDW

## Slide 5: How do you get there?

## Slide 6: Sorting of CDW  valuable resources

## Slide 7: Can you and are you allowed to use CDW mineral fraction in construction?

## Slide 8: CDW as concrete aggregate
8/16 2/8 0/2
Recycled aggregates from the CDE recycling centre outside Marseille, southern France
(fraction limits in mm)

## Slide 9: CDW as concrete aggregate
Regulated in EN 206:2013+A1:2016 (Concrete) and EN 12620+A1:2008 (Aggregates for concrete):
applies to concrete mixed on site, ready-mixed or produced in a plant for precast concrete products
Harmonized in EU  CE-marked
System 2+  certificate by notified body
General requirements:
Properties as for virgin aggregates
Aggregate should be considered Alkali-Silica Reactive (ASR), until opposite proven
Water soluble sulfates: ≤ 0.7 wt%
Classification of constituents of coarse recycled aggregates, following EN 933-11:2009
Dangerous substances: emission of radioactivity, release of heavy metals, release of polycyclic aromatic hydrocarbons

## Slide 10: Classification of constituents of coarse RA (following EN 933-11)

## Slide 11: CDW quality – EN 206:2013
 | Class | Rc (concrete) | Rc+Ru (concrete + unbound) | Rb (brick) | Ra (bituminous) | Fl (floating material) | XRg (glass, others)
EN 206 | Type A | ≥ 90% | ≥ 95% | ≤ 10% | ≤ 1% | ≤ 2% | ≤ 1%
 | Type B | ≥ 50% | ≥ 70% | ≤ 30% | ≤ 5% | ≤ 2% | ≤ 2%

## Slide 12: CDW quality – EN 206:2013+A1:2016 and limits on use
High sorting ambitions  higher aggregate quality  higher economic value

## Slide 13: CDW quality – new proposal
Property | Type A+ | Type A | Type B | Type L
Density (oven dry) [kg/m3] | > 2000 | > 2000 | > 2000 | ≤ 2000 (To be declared)
Rc+Ru [%] | ≥ 95 % | ≥ 90 % | ≥ 70 % | ---
Rb [%] | ≤ 5 % | ≤ 10 % | ≤ 30 | ---
Rc+Ru+Rb [%] | --- | ---- | ≥ 90 % | ≥ 95 %
Ra [%] | ≤ 1 % | ≤ 5 % | ≤ 10 % | ≤ 5 %
FL | ≤ 0,2 % | ≤ 2 % | ≤ 2 % | ≤ 5 %
X+Rg [%] | ≤ 1 % | ≤ 5 % | ≤ 5 % | ≤ 5 %
Shape | ≤ FI35 or ≤ SI40 | ≤ FI50 or ≤ SI55 | To be declared | To be declared
Water soluble sulfates | ≤ SS0,2 | ≤ SS0,2 | ≤ SS0,2 | ≤ SS0,2
Influence on setting time | ≤ A10 | ≤ A40 | ≤ A40 | ≤ A40
Water absorption | ≤ 5% | ≤ 10 % | To be declared | To be delared

## Slide 14: How does the CDW quality affect concrete performance?

## Slide 15: CDW quality assessment
 | CDW used |  | Quality class requirements | 
Material | SE B4 | UK B1 | EN 206 A/B | RE4 A+ / A / B / L
Rc [%] – concrete | 71 | 13 | ≥90/50 | 
Ru [%] – unbound stones | 27 | 76 | --- | 
Rc+Ru [%] | 98 | 89 | ≥95/70 | ≥95/90/70/---
Rb [%] – bricks, tiles | 1 | 3 | ≤10/30 | ≤5/10/30/---
Rc+Ru+Rb [%] | 99 | 92 |  | ---/---/≥90/95
Ra [%] – bituminous material | 0 | 7 | ≤1/5 | ≤1/5/10/5
Fl [cm3/kg] – floating particles | 0.1 | 0.2 | ≤2/2 | ≤0.2/2/2/5
X+Rg [%] – Others + glass | 0 | 0.2 | ≤1/2 | ≤1/5/5/5
Quality class according to EN 206 | B | --- |  | 
Quality class according to RE4 | A+ | B |  | 

## Slide 16: Quality vs replacement level – example from HPC
 | CDW |  | % coarse aggregate (2-8 or 4-10) |  |  |  |  | Compressive strength (N/mm2) |  |  | 
Name | Source | % |  | w/b ratio | binder amount | T500 (s) | Flow (mm) | 16 h | 1 d | 7 d | 28 d
HPC-6-1 | SE | 90 | 75 | 0.30 | 655 | 5.8 | 515 |  | 42 | 67 | 75
HPC-7-1 | SE | 90 | 65 | 0.30 | 655 | 5.5 | 538 |  | 46 | 66 | 76
HPC-8-1-1 | SE | 90 | 75 | 0.30 | 655 | 3.5 | 618 |  | 41 | 62 | 74
HPC-9-1-1 | SE | 90 | 65 | 0.30 | 655 | 2.1 | 603 |  | 43 | 63 | 76
HPC-9-1-2 | SE | 90 | 65 | 0.31 | 655 | 2.2 | 743 |  | 34 | 57 | 71
HPC 10-3 | UK | 90 | 55 | 0.28 | 655 | 4.1 | 575 |  | 26 | 44 | 53
HPC 10-6 | UK | 90 | 55 | 0.27 | 655 | 7 | 518 |  | 28 | 48 | 61
HPC 10-8 | UK | 90 | 55 | 0.29 | 720 | 1 | 758 |  | 12 | 48 | 60
HPC 10-10 | UK | 90 | 55 | 0.28 | 720 | 3 | 598 |  | 19 | 51 | 63
HPC 10-12 | UK | 50 | 50 | 0.29 | 655 | 6.2 | 598 |  | 23 | 58 | 
HPC 10-13 | UK | 60 | 60 | 0.29 | 655 | 2.9 | 645 |  | 20 | 57 | 65
HPC 10-16 | UK | 50 | 50 | 0.29 | 725 | 1.8 | 620 |  | 32 | 54 | 74
HPC 10-18 | UK | 50 | 50 | 0.26 | 725 | 2.6 | 638 |  | 35 | 54 | 74
HPC 10-19 | UK | 50 | 50 | 0.28 | 725 | 1.4 | 655 |  | 33 | 58 | 73
HPC 10-20 | UK | 50 | 50 | 0.27 | 725 | 6 | 563 |  | 38 | 62 | 71
Reference values (industrial partner) |  |  |  |  |  |  | 700 | 15 | 27 | 45 | 

## Slide 17: CDW quality – proposal on new limits
Type of CDW | Exposure classes |  |  |  |  | 
 | X0, (XC1?) | (XC1?), XC2, XS1, XD1, XS1, XA1 | XC3, XC4 | XS2, XS3, XD2, XD3 | XF2, XF3, XF4 | XF4
Type A+ | 100 % | 30 % | 30 % (1 | 30 % (2 | 30 % (3 | 30 % (4
Type A | 100 % | 20 % | 20 % ( 1 | 20 % (2 | 20 % (3 | 20 % (4
Type B (5 | 100 % | 20 % | 0 % | 0 % | 0 % | 0 %
Type L (5 | 100 % | 20 % | 0 % | 0 % | 0 % | 0 %
Sufficient carbonation resistance of the concrete shall be verified Sufficient chloride resistance of the concrete shall be verified Sufficient frost resistance of the aggregate shall be verified Sufficient salt-frost resistance of the concrete shall be verified Type B and L is mainly intended for non-structural concrete. They shall not be used in concrete with compressive strength > C30/37. |  |  |  |  |  | 

## Slide 18: Sandwich element production – upscaling at Creagh Concrete

## Slide 19: Sandwich element testing – accelerated weathering (ACCIONA)
Four-point bending test of Sandwich panel 3
Load-displacement curve of sandwich panel 3

## Slide 20: Sandwich element testing – accelerated weathering (ACCIONA)
Panels 1 & 2: 1 month accelerated weathering
Panels 3 & 4: reference

## Slide 21: Sandwich element testing – accelerated weathering (ACCIONA)
Panels 1 & 2: 1 month accelerated weathering
Panels 3 & 4: reference
No significant differences between panels subjected to accelerated weathering and those not exposed!

## Slide 22: Final remarks (part 1)
Development of materials constituting high levels of CDW aggregates: vibrated concrete (OPC and AAB based), SCC, HPC, lightweight concrete, earth plaster and mortar, rammed earth, …
Development and industrial scale production (upscaling from lab) of a range of components and elements 
Concrete prefab elements based on SCC and/or HPC, and in some cases vibrated concrete

## Slide 23: Final remarks (part 2)
Work on CDW aggregate characterization illustrates importance of the CDW quality and a robust quality assessment system  ambition level for aggregate replacement
Results confirm the high flexibility of the RE4 approach, with a minimum replacement level at 50 %, even in the industrial environment (TRL7)
Modification of laboratory mix design to industry scale, restricted to small changes in amount of SPs (using different virgin aggregates, cement type, additives)
The campaign revealed some challenges:
  need of adoption to variations in CDW quality
  difficulties working with two-layer textile reinforcement on industrial scale
On overall it was very successful, paving the way for a reliable use of high ratios of CDW in the prefabrication industry!

## Slide 24: Thanks to partners for great cooperation!

## Slide 25: Thank you for your attention
Linus Brander
Linus.Brander@ri.se
Insert company logo