## Slide 1: Materials development and characterization
Prof Glikeria Kakali, NTUA

## Slide 2
Objectives:
exploit CDW streams as raw materials, constituents, reinforcing/functional agents in GI panel
improve the performance of GI layers through the incorporation of CDWs
characterize CDWs and final products
plastics
textiles
wood
bricks
glass
EPS
PU
concrete
cement
Al/stainless steel scrap
wood fibers
plastic fibers
textile fibers
geopolymer
insulation layer
MOC
PCMs aggregates
adhesive
Al frame
green wall cassette
plant substrate
10 CDWs were used for developing 11 products to be incorporated in GI panel
Involved partners: NRGIA, LEITAT, CID, UBRUN, NTUA, COLL, ALCN, Cnano

## Slide 3: PE Fibers
Processing (addition of plasticizer)
Extrusion
Spinning
Cutting
Pellets from CDW
Properties | 
Length (mm) | 6-12
Aver. Diameter (μm) | 59.4
Density (g/cm3) | 0.97
Tensile Modulus (MPa) | 258.60
PE fibers
8.5 kg
geopolymer layer
(UBRUN/NTUA)
Processing

## Slide 4: Wood Fibers
Filtration and washing
1
2
3
4
5
Dried (60oC overnight)
Obtaining individual fine fibers by mechanical treatment
MDF chips
MDF pulp
MDF fibers dried
Fiber blocks
Fine fibers
20 kg
MOC layer (UBRUN)
PU layer (CID)
Average length (μm) | Mean diameter (μm) | Fines content (%)
263 ± 16 | 21.6 ± 0.4 | 41.7 ± 3.2
Hydrothermal treatment
(95oC, 30 min)
Morphological analysis
Processing

## Slide 5: Textile Fibers
Washing
Cutting
1
2
3
4
1st Grinding
Textiles as received
Fibers obtained after 1st Grinding
6.5 kg
Substrate in green wall (ALCN)
Fibers obtained after 2nd Grinding

## Slide 6: Geopolymer layer
Precast component
Comp. strength: 43 MPa
Flex. strength: 4 MPa
Density: 2 g/cm3
CDW content: 91% w/w
Lightweight component
Comp. strength: 15 MPa
Flex. Strength: 3.2 MPa
Density: 1.3 g/cm3
CDW content: 92% w/w

## Slide 7
Geopolymer layer showing warping/cracking
Final geopolymer layer
Properties |  |  | 
Specific Heat (kJ/kg∙°C) | 0.9 | Compressive Strength (MPa) | 15.3
Thermal Conductivity (W/m.K) | 0.45 | Water absorption (%) | 4.1
Density (kg/m3) | 1300 | Sorptivity (mm/min2) | 0.18
Poisson's Ratio | 0.11 | Wet – dry cycles | Stable
Young's modulus (GPa) | 1.3 | Flammability | inflammable
Tensile Resistance (MPa) | 3.2 | CDW content (wt. %) | 88
Issues due to the dimensions of the layers
drying shrinkage warping/cracking
increase fiber length add 6% CAC
from 6 to 12 mm cure under lid
COOLH
12.5 m2/240 Kg

## Slide 8: PU foam layer
1st approach: produce fresh PU from recycled PU
too high density
too low mechanical properties
2nd approach: use pristine PU – use CDWs as fillers
PU foam
 | Soft | Rigid
CDW PU foam (%) | 1.5 | 0
CDW Wood fibers (%) | 0 | 2
Density (kg/m3) | 24 | 46
Compression Strength (MPa) | 0.015 | 0.113
Tensile strength (MPa) | 0.023 | 0.239
Young Modulus (MPa) | 0.518 | 2.919
Thermal Conductivity (W/m.K) | 0.0338 | 0.024
COOL/AVR
95 m2/85 kg
wood fibers

## Slide 9: Magnesium Oxychloride Cement (MOC)
Properties | 
Compressive strength (MPa) | 41.9
Tensile strength (MPa) | 10.4
Young's modulus (GPa) | 2.7
Density (kg/m3) | 1050
Thermal conductivity (W.m-1.°C-1) | 0.31
20% w/w CDW content
(aggregates, fibers, saw dust)
COOL/AVR
130 kg

## Slide 10: Aggregates with PCMs
Properties | Values
Bulk density (g/cm3) | 0.8
Water absorption (% wt.) | 0.05
Mass loss (% wt) | 1.8
Thermal conductivity (W/m.K) | 0.141
Heat storage capacity before thermal cycling (J/g) | 23.7
Heat storage capacity after thermal cycling | 21.2
50% w/w CDW content
(concrete aggregates)
MOC layer
19 kg

## Slide 11: Structural adhesive
Properties | L2520/2C | GI/2C
Viscosity | 10000 cps | 100000 cps
Mixing ratio with CTZ GI17 | 4 to 1 | 4 to 1
Pot Life of the mixture | 40 min | 30 min
Minimum Pressing Time | 4 h | 3 h
Tensile Strength (single lap shear test) | 8.2 MPa | 23.3 MPa
Shore D | 50 | 85
Final Hardening Time (2mm thickness) | 24 h | 24 h
VOC | < 0.1 | < 0.1
CDW content (cement powder) : 62% w/w
CID
7.5 kg

## Slide 12: Photocatalytic Paint
TiO2/SiO2 nanopowder doped with thiourea
Synthesis of
photocatalytic powder
Synthesis of
paint
Ingredients | water | Kronos 2360 | fillers | additives | Cnano powder
% w/w | 27.2 | 15 | 29 | 23.8 | 5
up scaling
ACCIO/STRESS
4 L

## Slide 13: Extrusion/casting of geopolymer and MOC

## Slide 14: Characterization of materials
Measurement database
http://www.greeninstruct.eu/technology-transfer/
Info Part
list of samples
techniques
Instrumentation
measurement conditions
Measurement Part
Raw measurement files
open access
Available upon request
7 partners
27 techniques
454 samples

## Slide 15: CDW content in GI panel
INTERNAL + EXTERNAL PANEL |  |  |  |  |  | 
 | GREEN WALL WITH ALUMINIUM FRAME |  |  | GREEN WALL WITH SS FRAME |  | 
Material | Weight (kg/m2) | CDW content (%) | CDW (kg/m2) | Weight (kg/m2) | CDW content (%) | CDW (kg/m2)
Internal panel | 95.04 | 65 | 61.56 | 95.04 | 65 | 61.56
Green wall | 82.27 | 98 | 80.62 | 85.15 | 95 | 80.89
TOTAL | 177.31 |  | 142.18 | 180.19 |  | 142.45
CDW in panel (%) | 80 |  |  | 79 |  | 

## Slide 16: Conclusions
10 CDW streams were valorized as raw materials, constituents, reinforcing/functional agents in GI panel
plastics, textiles, wood, bricks, glass, EPS, PU, concrete, cement, Al/stainless steel scrap
fibers, geopolymers, insulation layer, MOC, PCMs aggregates, adhesive, frame, green wall cassette, plant substrate
11 products were developed and incorporated in the GI panel
The GI panel contains 80% w/w CDWs

## Slide 17: Thank you for your attention
Dr Glikeria Kakali
kakali@central.ntua.gr