## Slide 1: GREEN INtegrated STRUCTural Elements for Retrofitting and New Construction of Buildings
Xiangming Zhou, Brunel University London

## Slide 2: Where are we? Who are we?
Students: ~16,000
Staff: ~ 2,600
Colleges: 3
Named after the great Victorian engineer Isambard Kingdom Brunel

## Slide 3: Project information
    Call identifier: NMBP EeB-04-2016
Project number | 723825
Project value | 5.0 million €
Starting month | October 2016
Project Duration | 42 months
Our consortium

## Slide 4: EeB-04-2016 Call Background
    NMBP EeB-04-2016: New technologies & strategies for the development of pre-fabricated elements through the reuse & recycling of construction materials & structures
        “In EU, CDW accounts 25-30% of all waste generated”
        “demands large-scale re-use & recycling of CDW in construction industry”
        “CO2 & energy reduction”
        “pre-fabricated components to reduce costs & to facilitate installation/dismantling & re-use of components”
        “recovery/ recycling of materials that have the highest technical and economic interest and which are associated to refurbishment or demolition processes”
        “reuse different materials in energy-efficient buildings”
        “the development of processes for easy disassembly”
        “address strict regulations & standards (e.g. anti-seismic) in several European regions”
        “optimization of recyclability properties through the uptake by the manufacturing chain”
        Etc.

## Slide 5: Main objectives
Efficient, robust, eco-friendly and replicable processes
Cost efficient products and new supply chains
Safe and energy efficient buildings
Comfortable, healthy and productive environment
Sustainability and cost savings through CDW sourced materials & C2C

## Slide 6: Expected impacts
High CO2 and energy inputs savings during the fabrication and operation processes
High rates of CDWs recycled and reused during building blocks fabrication
Re-entry into production lines with coherent design strategies
Incorporation of the safety-by-design approach
Reduction of uncertainty linked to the use of recycled products

## Slide 7: Green INSTRUCT at a glance

## Slide 8: Main innovations
Prefab structural building block suitable both for retrofitting as well as new construction
>70% per weight of CDW
U-value of 0.14 W/m2ºC
Acoustic insulation in the 55-60dB
Vertical Green Wall
Continuous manufacturing using extrusion

## Slide 9: Highlight of the achievements
Innovative panel design,
Connection, assembly, replacement & dismantle

## Slide 10: Highlight of the achievements
A clear collection, separation, sorting and characterisation strategy

## Slide 11: Highlight of the achievements

## Slide 12: Highlight of the achievements
Manufactured fibres from CDW (plastic, textile, wood) for reinforcing geopolymer, MOC, PU, structural adhesive etc.
Extruded PU fibres
Recycled textile fibres
Recycled wood fibres

## Slide 13: Highlight of the achievements
Magnesium Oxychloride (MOC) cement with sawdust and PCM aggregates

## Slide 14: Highlight of the achievements
Rigid and soft PU Foam with inclusion of waste PU foam and waste wood fibres
Hard PU Foam |  |  |  |  | 
Wood fibres | Density (g/cm3) | Compression Strength | Tensile strength |  | Thermal conductivity
 |  | Em (MPa) at 10% | Young modulus (MPa) | Max. Resist. (MPa) | Lambda (w/m∙K)
2% | 0.0241 | 0.0157 |  |  | 0.03395
Soft PU Foam |  |  |  |  |  | 
PU foam (CDW) | Density (g/cm3) | Compression Strength | Tensile strength |  | Thermal conductivity | 
 |  | Em (MPa) at 10% | Young modulus (MPa) | Max. Resist. (MPa) |  | Lambda (w/m∙K)
1.5% | 0.0247 | 0.0148 | 0.518 | 0.023 | 0.03383 | 

## Slide 15: Highlight of the achievements
Bulk density (g/cm3) | 0.8
Water absorption (% wt.) | 0.05
Mass loss (% wt) | 1.8
Thermal conductivity (W/mK) | 0.141
Heat storage capacity before thermal cycling (J/g) | 23.7
Heat storage capacity after thermal cycling | 21.2
PCM-impregnated aggregates

## Slide 16: Highlight of the achievements
lightweight geopolymer from CDW (88 wt%)
Hydrothermal process to convert waste glass into activation solution with 81% conversion rate
Properties | EPS+PE
Specific Heat (KJ.Kg-1.°C-1 ) | 0.9
Thermal Conductivity (W.m-1.°C-1) | 0.45
Density (Kg.m-3) | 1400
Emissivity | 0.9
Poisson's Ratio | 0.11
Young's modulus (GPa) | 1.3
Tensile Resistance (MPa) | 3.2
Compressive Resistance (MPa) | 15.3

## Slide 17: Highlight of the achievements
CDW content (cement powder) : 62% w/w

## Slide 18: Highlight of the achievements
Successful extrusion and casting of Geopolymer panels and aluminium profiles

## Slide 19: Highlight of the achievements
25 m2 of green façade area needed to clean 1 m3 of greywater/day
Innovative green wall design with substrate & cassette from CDW

## Slide 20: Highlight of the achievements
Optimised CFD modelling has achieved a U-value = 0.13 W/m2K and sound insulation performance of 57 dB

## Slide 21: Highlight of the achievements
Developed a photocatalytic paint used for coating the MOC layer using doped TiO2 nanoparticles with optimized loading and low agglomeration. The coating is harmless to human health and effectively improve indoor air quality.

## Slide 22: Highlight of the achievements
Demosntration

## Slide 23: Thank you for your attention
Presenter name: Xiangming Zhou
Presenter email:
Xiangming.Zhou@brunel.ac.uk